## Slide 1: Connecting Atomistic Simulations and Experiments Using Virtual Diffraction
Shawn P. Coleman
Lightweight and Specialty Metals Branch, ARL

## Slide 2: Motivation
Radial Distribution Functions
  Identification of complex material (non-cubic) phases and phenomena within atomistic simulations is difficult.
  Experimental x-ray and electron diffraction routinely used for characterization of (complex) materials.
Fundamental disconnect between simulation and experimental characterization tools.
Santos et al. (2000)
Ollivier et al. (1997)
XRD
of Alumina Phases
SAED and HRTEM
of 120° twins in κ-Al2O3
z
  Virtual diffraction offers a bridge to directly connect atomistic simulations with experimental characterization.
θ
α
γ
κ
Centrosymmetry(Å2)
0
20
5
10
15
Alumina Polymorphs

## Slide 3: Background
Twist boundaries in Au
C
B
Experimentally Observed
Computed Structure Factor
(Bristowe and Sass, 1980)
Nanocrystaline Ni
5 nm
12 nm
(Derlet et al, 2005)
Debye Scattering Equation
Required knowledge of crystal structure.
Produced only XRD patterns
Limited Implementation
  Previous studies have paved the way to the current virtual diffraction algorithm and implementation:
D
E

## Slide 4: Virtual Diffraction from 10,000 ft
Compute diffraction intensities at each point on the reciprocal space mesh using the structure factor equations
  Compute structure factor for all atoms within the simulation.
3. Analysis and visualization of diffraction intensities to produce
    X-ray diffraction line profiles (XRD)
  Selected area electron diffraction patterns (SAED)
Create a mesh of reciprocal space
    3D rectilinear mesh but with spherical boundary conditions.
    Ultrafine resolution eliminates any need for prior knowledge of the crystal structure.
Implemented into the LAMMPS MD code

## Slide 5: Diffraction Intensity Computation
All atoms are sampled at each reciprocal point.
At each reciprocal lattice node the diffraction intensity is calculated utilizing the structure factor equation,
Sampled Reciprocal Space
Structure Factor:
~10-100M
Relp
~1-10M Atoms
= Lorentz-Polarization Factor (only XRD)
= Structure Facture
= Reciprocal Lattice Point (Relp)
= Number of Atoms in Simulation
= Atomic Scattering Factor
= Atom Position

## Slide 6: Computational Optimization
MPI parallelization over real space
  LAMMPS - Spatial decomposition of atoms parallelized over MPI processes
  Each process must have a copy of
  the reciprocal space mesh
4
5
6
7
0
1
2
3
CPU
Very Memory Intensive
~10-100M Relp
~1-50M Atoms

## Slide 7: Multilevel Parallelization
OpenMP parallelization of reciprocal space
  Reduce the number of MPI processes per node
  Decompose reciprocal space with OpenMP
  MPI Parallelization of atoms across
  multiple CPU nodes
CPU
0
OpenMP threads
4
5
6
7
0
1
2
3
~10-100M Relp
~1-50M Atoms
0
OpenMP threads
4
5
6
7
0
1
2
3
0
OpenMP threads
4
5
6
7
0
1
2
3
0
OpenMP threads
4
5
6
7
0
1
2
3
Preventative for MD computations

## Slide 8: Heterogeneous Computing
Using MIC accelerators in addition to CPU
  Offloading a percentage of the computation for concurrent computation of intensity.
4
5
6
7
0
1
2
3
CPU
MIC
4
5
6
7
0
1
2
3
0-3
4-7
8-11
12-15
16-19
20-23
24-27
28-31

## Slide 9: 3D Diffraction Data
Example 3D diffraction data taken from Ni tilt grain boundary.
How to visualize 3D diffraction data to represent experimental techniques and make unique insights?

## Slide 10: Analysis and Visualization
100
  Diffraction Theory
  Diffraction conditions satisfied when a reciprocal lattice node is located on the surface of Ewald’s sphere
  X-Ray Powder diffraction patterns
  All orientations of the crystal equally possible
  Intensity data are binned corresponding to their diffraction angle calculated using Bragg’s law:
  Concentric spherical shell bounding angles
  Electron diffraction patterns
  Radius of Ewald sphere much larger
  Diffraction conditions intersect a near planar slice of reciprocal space lattice
b3
b2
b1
origin
100
300
310
b3
b2
b1
Electron Diffraction
X-Ray Diffraction
origin
300
310
30°
0°
60°
90°
120°
150°
180°
b1
origin
100
1/λ
1/λ

## Slide 11: Check – Al Twist GBs
Virtual SAED patterns clearly identify misorientation in Al {111} twist GBs.
Secondary peaks emerge due to screw dislocation network.
Aluminum Twist Grain Boundaries

## Slide 12: Bulk Alumina
Verwey (1935)
Husson (1996)
Virtual x-ray diffraction patterns can successfully differentiate alumina polymorphs.
Virtual XRD patterns can be compared directly to experiments to validate the fidelity of the potential – ReaxFF.
  Al2O3 Polymorphs
θ
α
γ
κ
  X-ray Diffraction
A generic tool for structural identification in simulations of complex materials.
Coupled with optimization routine, can become a route to provide atomic resolution of experimental diffraction patterns – including defects.
Ollivier (1997)
Ishizawa (1979)
Intensity
Intensity
Intensity
Intensity

## Slide 13: Alumina Surfaces
Virtual SAED patterns can verify the correct orientation of surface simulations.
θ-Al2O3 (110) Surface
α-Al2O3 (0001) Surface
Virtual SAED identify substantial surface reconstructions still have underlying structure.
Providing atomic detail to smearing of diffraction peaks can help associate to specific strain field.
Tracking ‘motion’ of peaks to identify phase transformation mechanisms.

## Slide 14: Alumina Interfaces
Virtual SAED patterns help identify misorientation in Al2O3 GB simulations.
Simulated patterns are matched to experimental (when available) to provide further validation of the structure.
α-Al2O3 Basal Twin Boundary
Virtual SAED patterns aided the construction of complex interfaces.
Optimal orientation relationship evaluated by overlapping diffraction peaks.

## Slide 15: α-Al2O3 (0001) / Al (111) Orientation Relationship
α-Al2O3 (0001)
Al (111)
Interface
Modeled interface SAED pattern by overlapping SAEDs from each grain.
Lower interface energy found at maximum overlapping diffraction peaks.

## Slide 16: α-Al2O3 (0001) / Al (111)
z
x
Medlin (1997)
z
x
  Work of adhesion using ReaxFF agree with DFT prediction
  Initial - 0.40 J/m2
  Optimized - 0.82 J/m2
  DFT: 1.06 J/m2 Siegel (2002)
  Optimized orientation SAED agrees with experimental.
Initial Orientation
Optimized Orientation

## Slide 17: Wrap Up
Conclusions
Implementation of XRD and SAED virtual diffraction methods open new routes for greater coupling between experiments and simulations.
Designed to be sufficiently generic for any material system and is adaptable to multimillion atom simulations.
Future Outlooks
Nanocrystalline Metals
Using virtual diffraction to identify mechanisms of phase transformation and grain growth.
Investigating the coupling between simulation length scales using peak broadening.
Thank You